# Multi-Stage Structural Transformations in Zero-Strain Lithium Titanate Unveiled by
                    <i>in Situ</i>
                    X-ray Absorption Fingerprints

Wei Zhang et al. (2017)
DOI: 10.1021/jacs.7b07628
Category: electrochemistry | Element: Ti | Edge: K
5 condition(s)

Please review each condition and mark Correct / Incorrect.

# Condition 1: Pristine lithium titanate (Li4/3Ti5/3O4) electrode

| Category | electrochemistry |
| --- | --- |
| Phases & Fractions | Li4/3Ti5/3O4: 1.0 |
| Reasoning | At the pristine state (OCV, 2.50 V) before any electrochemical discharge (lithiation), the lithium concentration x is 0.0. No lithium has intercalated into the structure, meaning the material remains entirely in its initial Li4/3Ti5/3O4 phase with titanium exclusively in the Ti4+ oxidation state. |
| Correct? | Yes / No — Comments: |

Stage 1 Prompt (what the LLM sees):

## Sample Information

- **Material**: Pristine lithium titanate (Li4/3Ti5/3O4) electrode

- **Application/Context**: Lithium-ion battery

## Electrode / Cell Details

- **Electrode type**: working electrode

- **Active material**: Li4/3Ti5/3O4

- **Electrolyte**: EC/DMC/LiPF6 (1:1:1)

- **Cell type**: in-situ coin cell

## Electrochemical Conditions

- **Charge/discharge state**: OCV

- **C-rate**: not reported

- **Voltage**: 2.50 V

- **State of charge**: Li concentration x = 0.0

- **Cycle number**: 1

- **Capacity**: not reported

## Sample-Specific Conditions

- Li concentration x = 0.0

- in-situ

- Pristine electrode before discharge

## Measurement

We plan to measure the Ti K XANES spectrum of this electrode.

## Questions

Based on ALL the electrochemical conditions above:

1. What phases (oxidation states / compounds of Ti) could exist in this electrode at this state?

2. How many of these phases are significant (>5% fraction)?

3. For each significant phase, estimate its fraction (fractions should sum to 1.0).

4. What reference spectra should be prepared for linear combination fitting?

5. What scientific reasoning connects the specific electrochemical conditions to your predicted phases and fractions?

# Condition 2: Lithium titanate, Li4/3Ti5/3O4, electrode

| Category | electrochemistry |
| --- | --- |
| Phases & Fractions | Li4/3Ti5/3O4: 0.92, Li7/3Ti5/3O4: 0.08 |
| Reasoning | During the initial stages of lithiation (x <= 0.5), lithium intercalation into zero-strain Li4/3Ti5/3O4 proceeds via a quasi-solid solution mechanism rather than an immediate macroscopic two-phase reaction. At x=0.5, the system is at the end of this quasi-solid solution regime. Consequently, the pristine Li4/3Ti5/3O4 phase fraction decreases very slowly and remains highly dominant (92%), while only a small fraction (8%) of the fully lithiated Li7/3Ti5/3O4 phase has formed. This strongly deviates from a simple linear two-phase reaction model which would incorrectly predict a 50/50 mixture at x=0.5. |
| Correct? | Yes / No — Comments: |

Stage 1 Prompt (what the LLM sees):

## Sample Information

- **Material**: Lithium titanate, Li4/3Ti5/3O4, electrode

- **Application/Context**: Lithium-ion battery

## Electrode / Cell Details

- **Electrode type**: working electrode

- **Active material**: Li4/3Ti5/3O4

- **Electrolyte**: EC/DMC/LiPF6 (1:1:1)

- **Cell type**: in-situ coin cell

## Electrochemical Conditions

- **Charge/discharge state**: discharging

- **C-rate**: C/10

- **Voltage**: not reported

- **State of charge**: Li concentration x = 0.5

- **Cycle number**: 1

- **Capacity**: not reported

## Sample-Specific Conditions

- Li concentration x = 0.5

- Measurement mode: in-situ

- First discharge cycle

## Measurement

We plan to measure the Ti K XANES spectrum of this electrode.

## Questions

Based on ALL the electrochemical conditions above:

1. What phases (oxidation states / compounds of Ti) could exist in this electrode at this state?

2. How many of these phases are significant (>5% fraction)?

3. For each significant phase, estimate its fraction (fractions should sum to 1.0).

4. What reference spectra should be prepared for linear combination fitting?

5. What scientific reasoning connects the specific electrochemical conditions to your predicted phases and fractions?

# Condition 3: Lithium titanate (Li4/3Ti5/3O4) electrode

| Category | electrochemistry |
| --- | --- |
| Phases & Fractions | Li4/3Ti5/3O4: 0.77, Li7/3Ti5/3O4: 0.23, outside_references: True |
| Reasoning | During electrochemical discharge, Li intercalation into Li4/3Ti5/3O4 proceeds via a multi-stage kinetic pathway rather than a simple macroscopic two-phase reaction. At early stages (x <= 0.5), it forms a quasi-solid solution where the pristine phase fraction decreases very slowly. At x = 0.6, the system has just entered the intermediate stage (0.5 < x < 0.87) of rapid macroscopic phase separation. Because of the delayed phase transformation from the initial quasi-solid solution stage, the fraction of the pristine Li4/3Ti5/3O4 phase remains unusually high (0.77) compared to what a simple linear lever rule would predict (which would be 0.40 pristine at x=0.6). |
| Correct? | Yes / No — Comments: |

Stage 1 Prompt (what the LLM sees):

---

## Sample Information

- **Material**: Lithium titanate (Li4/3Ti5/3O4) electrode

- **Application/Context**: Lithium-ion battery

## Electrode / Cell Details

- **Electrode type**: working electrode

- **Active material**: Li4/3Ti5/3O4

- **Electrolyte**: EC/DMC/LiPF6 (1:1:1)

- **Cell type**: in-situ coin cell

## Electrochemical Conditions

- **Charge/discharge state**: discharging

- **C-rate**: C/10

- **Voltage**: not reported

- **State of charge**: x = 0.6 (Li concentration)

- **Cycle number**: 1

- **Capacity**: not reported

## Sample-Specific Conditions

- Li concentration x = 0.6

- Measurement mode: in-situ

- Electrode discharged to x=0.6 during two-phase transformation

## Measurement

We plan to measure the Ti K XANES spectrum of this electrode.

## Questions

Based on ALL the electrochemical conditions above:

1. What phases (oxidation states / compounds of Ti) could exist in this electrode at this state?

2. How many of these phases are significant (>5% fraction)?

3. For each significant phase, estimate its fraction (fractions should sum to 1.0).

4. What reference spectra should be prepared for linear combination fitting?

5. What scientific reasoning connects the specific electrochemical conditions to your predicted phases and fractions?

---

# Condition 4: Lithium titanate (Li4/3Ti5/3O4) electrode

| Category | electrochemistry |
| --- | --- |
| Phases & Fractions | Li4/3Ti5/3O4: 0.13, Li7/3Ti5/3O4: 0.87 |
| Reasoning | During electrochemical discharge (lithiation) of Li4/3Ti5/3O4, the system undergoes a multi-stage phase transformation. It initially forms a quasi-solid solution (x <= 0.5) before undergoing a macroscopic two-phase separation. At a lithium concentration of x=0.87, the system is in the two-phase region and intersects the ideal two-phase line. Therefore, the phase fraction of the fully lithiated end-member (Li7/3Ti5/3O4) directly corresponds to the lithium concentration (0.87), leaving 0.13 of the pristine Li4/3Ti5/3O4 phase. |
| Correct? | Yes / No — Comments: |

Stage 1 Prompt (what the LLM sees):

## Sample Information

- **Material**: Lithium titanate (Li4/3Ti5/3O4) electrode

- **Application/Context**: Lithium-ion battery

## Electrode / Cell Details

- **Electrode type**: working electrode

- **Active material**: Li4/3Ti5/3O4

- **Electrolyte**: EC/DMC/LiPF6 (1:1:1)

- **Cell type**: in-situ coin cell

## Electrochemical Conditions

- **Charge/discharge state**: discharging

- **C-rate**: C/10

- **Voltage**: not reported

- **State of charge**: 0.87

- **Cycle number**: 1

- **Capacity**: not reported

## Sample-Specific Conditions

- Li concentration x = 0.87

- Measurement mode: in-situ

- Electrode discharged to x=0.87, intersection with ideal two-phase line

## Measurement

We plan to measure the Ti K XANES spectrum of this electrode.

## Questions

Based on ALL the electrochemical conditions above:

1. What phases (oxidation states / compounds of Ti) could exist in this electrode at this state?

2. How many of these phases are significant (>5% fraction)?

3. For each significant phase, estimate its fraction (fractions should sum to 1.0).

4. What reference spectra should be prepared for linear combination fitting?

5. What scientific reasoning connects the specific electrochemical conditions to your predicted phases and fractions?

# Condition 5: Li4/3Ti5/3O4, working electrode

| Category | electrochemistry |
| --- | --- |
| Phases & Fractions | Li7/3Ti5/3O4: 1.0 |
| Reasoning | At a fully discharged state (x=1.0) and a voltage of 1.00 V, lithium intercalation into the zero-strain Li4/3Ti5/3O4 anode is complete. The multi-stage kinetic pathway has concluded, and the material has fully transformed into the lithiated end-member phase Li7/3Ti5/3O4, reducing the average Ti oxidation state from +4 to +3.4. |
| Correct? | Yes / No — Comments: |

Stage 1 Prompt (what the LLM sees):

## Sample Information

- **Material**: Li4/3Ti5/3O4, working electrode

- **Application/Context**: Lithium-ion battery

## Electrode / Cell Details

- **Electrode type**: working electrode

- **Active material**: Li4/3Ti5/3O4

- **Electrolyte**: EC/DMC/LiPF6 (1:1:1)

- **Cell type**: in-situ coin cell

## Electrochemical Conditions

- **Charge/discharge state**: discharged

- **C-rate**: C/10

- **Voltage**: 1.00 V

- **State of charge**: x = 1.0 (Li concentration)

- **Cycle number**: 1

- **Capacity**: not reported

## Sample-Specific Conditions

- Key variable: Li concentration x = 1.0

- Measurement mode: in-situ

- Fully discharged electrode

## Measurement

We plan to measure the Ti K XANES spectrum of this electrode.

## Questions

Based on ALL the electrochemical conditions above:

1. What phases (oxidation states / compounds of Ti) could exist in this electrode at this state?

2. How many of these phases are significant (>5% fraction)?

3. For each significant phase, estimate its fraction (fractions should sum to 1.0).

4. What reference spectra should be prepared for linear combination fitting?

5. What scientific reasoning connects the specific electrochemical conditions to your predicted phases and fractions?

Overall comments on this paper: ________________________________________